

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.2539/35/L/10 Date: 12th June, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. **Customer’s Details:** RESIDENT ENGINEER KeNHA NAIROBI REGION   **E-mail:** rd.nairobi@kenha.co.ke  **Address:** P.O Box 200- 00507 NRB Phone: 0713141871  **2. Customer Contact:** 0713141871 6. Job Card No.2475/S/2023  **3. Sample Description:** Lateritic Gravel 7. Date fee paid: 10/05/2023  **4. Sampled by:** CLIENT. 8. GOK MR No. 4052918  **5. Date Sample received:** 10/05/2023 9. Date Analysis started: 23/05/2023  **10. Additional information provided by the customer:** Outering Junction/Kangundo-Kamulu (B63) Road.   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | **TEST RESULTS** | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | **% Passing BS Sieve Size (mm)** | | | | | | **LL** | **PL** | **PI** | **LS** | **PM** | **MDD** | **OMC** | **4days Soak**  **(%)** | **Swell** | | **20** | **10** | **5** | **2** | **0.425** | **0.075** | **%** | **%** | **%** | **%** |  | **Kg/m3** | **( % )** | **(%)** | | 1938/S/22 | Gravel | 100 | 81 | 59 | 43 | 22 | 12 | 22 | 11 | 11 | 6 | 242 | 1930 | 8.0 | 55 | 0.2 | | **SOIL COMPOSITION: Gravel =57%, Sand =31%, Silt/clay =12%** | | | | | | | | | | | | | | | |

|  |
| --- |
|  |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC Soils Laboratory CSE Soils Laboratory**

**………………. …………………….**