

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.863/35/L/10 Date: 7th September, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **1. Customer’s Details:** WEBCON TECHNICAL SERVICES LIMITED  **E-mail:** webcontslimited@gmail.com  **Address:** P.O BOX 48151-00100 NRB Phone: 0720348930  **2. Customer Contact:** 0720348930 6. Job Card No. 1097/S/2023  **3. Sample Description:** Fill Material 7. Date fee paid: 26/10/2023  **4. Sampled by:** Client. 8. GOK MR No.4367952  **5. Date Sample received:** 26/10/2023 9. Date Analysis started:01/11/2023  **10. Additional information provided by the customer:** Oloosuyian -Kona Baridi Bridge.  **Source:** Kidemi Borrow pit     |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | TEST RESULTS | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T99** | | **CBR** | | | % Passing BS Sieve Size (mm) | | | | | | LL | PL | PI | LS | PM |  | OMC( % ) | 4days Soak  (%) | Swell(%) | | 20 | 10 | 5 | 2 | 0.425 | 0.075 | % | % | % | % |  | MDD Kg/m3 | | 687/S/23 | Fill Material | 100 | 91 | 85 | 77 | 61 | 45 | 36 | 24 | 12 | 6 | 732 | 1460 | 22.5 | 25 | 0.9 | | **SOIL COMPOSITION: Gravel = 23%, Sand = 32%, Silt/clay =45%** | | | | | | | | | | | | | | | |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC Soils Laboratory CSE Soils Laboratory**

**………………. …………………….**