

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.2547/35/L/10 Date: 15th June, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **1. Customer’s Details:** M/S PAMUCO BUILDERS LIMITED.  **E-mail: Not provided**  **Address:** P.O BOX 1857-00100 NRB **Phone:** 0724055813  **2. Customer Contact:**0724055813 6. **Job Card No.** 2658/S/2023  **3. Sample Description:** Gravel 7. **Date fee paid:** 02/06/2023  **4. Sampled by:** Client. 8. **GOK MR No**. 4053581  **5. Date Sample received:** 02/06/2023 9. **Date Analysis started**: 02/06/2023  **10. Additional information provided by the customer: PBC for the Maintenance of Ndenderu-Kamandura (B33) Road.**  **Source: Site Ruiru.**   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | TEST RESULTS | | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Dosage**% | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | % Passing BS Sieve Size (mm) | | | | | | LL | PL | PI | LS | PM |  | OMC (%) | 4days Soak  (%) | Swell (%) | | 20 | 10 | 5 | 2 | 0.425 | 0.075 | % | % | % | % |  | MDD  Kg/m3 | | 1060/S/22 | Gravel | Neat | 100 | 92 | 77 | 60 | 38 | 32 | 27 | 21 | 6 | 3 | 228 | 1790 | 14.2 | 30 | 0.3 | | **SOIL COMPOSITION: Gravel = 40%, Sand = 28%, Silt/clay =32%** | | | | | | | | | | | | | | | |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC Soils Laboratory CSE Soils Laboratory**

**………………. …………………….**