# 

# 

# **REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 554950/3/4 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: chiefengineer@mtrd.go.ke NAIROBI

Ref No. M.664/35/L/10 Date: 2nd October, 2023

|  |
| --- |
|  |

**1. Customer’s Details:** RESIDENT ENGINEER KURA.

**E-mail:** estherwa63@gmail.com

**Address:** P.O. Box 17956-00500 NRB **Phone:** 0721515815

**2. Customer Contact:** 0721515815 6. **Job Card No.** 841/S/2023

**3. Sample Description:**  Bottom Subgrade Layer 7. **Date fee paid:** 29/09/2023

**4. Sampled by:** MTRD Staff. 8. **GOK MR No**. 4367740

**5. Date Sample received:** 29/09/2023 9. **Date Analysis started**:29/09/2023

**10. Additional information provided by the customer:** Upgrading to Bituminous standard of Mariguini Housing project Roads (Road 2).

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Sample No.** | **Date tested** | **Chainage**  **(Km)** | **Position** | **Layer Thickness (mm)** | **Field dry density**  **Kg/m3** | **Field moisture content (%)** | **Max. dry density**  **T99**  **Kg/m3** | **Optimum moisture content (%)** | **Relative Compaction (%)** | **Relative moisture content (%)** |
| **Km 0+250-0+300 Road 2 Bottom subgrade Layer** | | | | | | | | | | |
| 409/S/23 | 29/09/23 | 0+270 | LHS | 150 | 1527 | 21.3 | 1527 | 21.0 | 100 | 101 |
| 410/S/23 | 29/09/23 | 0+400 | CL | 150 | 1575 | 20.9 | 1527 | 21.0 | 103 | 100 |
| 411/S/23 | 29/09/23 | 0+440 | RHS | 150 | 1583 | 21.7 | 1527 | 21.0 | 104 | 103 |
| 412/S/23 | 29/09/23 | 0+300 | CL | 150 | 1573 | 21.5 | 1527 | 21.0 | 103 | 102 |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC Soils Laboratory CSE Soils Laboratory**

**………………. …………………….**