

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.2585/35/L/10 Date: 21st June, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **1. Customer’s Details:** AUJAN INDUSTRIES LIMITED.  **E-mail: Not provided**  **Address:** P.O BOX 176-00610 NRB **Phone:** 0705052425  **2. Customer Contact:**0705052425 6. **Job Card No.** 2774/S/2023  **3. Sample Description:** Gravel 7. **Date fee paid:** 16/06/2023  **4. Sampled by:** Client. 8. **GOK MR No**. 4053687  **5. Date Sample received:** 16/06/2023 9. **Date Analysis started**: 16/06/2023  **10. Additional information provided by the customer: Construction of passenger platform lane in Nairobi commuter network.**  **Source: Athi River Quarry.**   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | TEST RESULTS | | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Dosage**% | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | % Passing BS Sieve Size (mm) | | | | | | LL | PL | PI | LS | PM |  | OMC (%) | 4days Soak  (%) | Swell (%) | | 20 | 10 | 5 | 2 | 0.425 | 0.075 | % | % | % | % |  | MDD  Kg/m3 | | 1091/S/22 | Gravel | Neat | 100 | 80 | 68 | 60 | 44 | 26 | 42 | 36 | 6 | 3 | 264 | 1683 | 17.1 | 30 | 0.3 | | **SOIL COMPOSITION: Gravel = 40%, Sand = 34%, Silt/clay =26%** | | | | | | | | | | | | | | | |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**