# 

# **REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.393/35/L/10 Date: 22nd August, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **1. Customer’s Details:** RESIDENT ENGINEER KeNHA  **E-mail:** rd.nairobi@kenha.co.ke  **Address:** P.O.BOX 200-00507 NAIROBI Phone: 0713141871  **2. Customer Contact:** 0713141871 6. Job Card No. 256/S/2023  **3. Sample Description:** Insitu Base Material 7. Date fee paid: 01/08/2023  **4. Sampled by:** Client. 8. GOK MR No.4058521  **5. Date Sample received:** 01/08/2023 9. Date Analysis started:01/08/2023  **10. Additional information provided by the customer:** Performance based contract for maintenance of Muthaiga-Kiambu B32 Road.  **SOURCE:** **5+350- 5+700 Shoulder.**     |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | TEST RESULTS | | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Dosage**% | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | % Passing BS Sieve Size (mm) | | | | | | LL | PL | PI | LS | PM | MDD Kg/m3 | OMC( % ) | 4days Soak  (%) | Swell(%) | | 20 | 10 | 5 | 2 | 0.425 | 0.075 | % | % | % | % |  |  |  | | **Improved with Simba Cem 1, 42.5N,7 Days Cure and 7 Days Soak** | | | | | | | | | | | | | | | | | |  | | 231/S/23 | **5+350-5+700** |  |  |  |  |  |  |  | 36 | 24 | 12 | 6 |  |  |  | 140 | <0.1 | |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**