

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.1783/35/L/10 Date: 22nd February, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. **Customer’s Details:** RESIDENT ENGINEER KURA   **E-mail:** estherwa63@gmail.com  **Address:** P.O Box 17956 00500 NRB Phone: 0721515815  **2. Customer Contact:** 0721515815 6. Job Card No.1775/S/2023  **3. Sample Description:** Gravel 7. Date fee paid: 16/02/2023  **4. Sampled by:** CLIENT. 8. GOK MR No. 4127586  **5. Date Sample received:** 16/02/2023 9. Date Analysis started: 17/02/2023  **10. Additional information provided by the customer:** PBC LOT 21 Reconstruction of Masai Lane.   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | **TEST RESULTS** | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | **% Passing BS Sieve Size (mm)** | | | | | | **LL** | **PL** | **PI** | **LS** | **PM** | **MDD** | **OMC** | **4days Soak**  **(%)** | **Swell** | | **20** | **10** | **5** | **2** | **0.425** | **0.075** | **%** | **%** | **%** | **%** |  | **Kg/m3** | **( % )** | **(%)** | | 717/S/22 | Gravel | 100 | 79 | 56 | 38 | 17 | 10 | 41 | 29 | 12 | 6 | 204 | 1612 | 17.8 | 30 | 0.9 | | **SOIL COMPOSITION: Gravel =62%, Sand =28%, Silt/clay =10%** | | | | | | | | | | | | | | | |

|  |
| --- |
|  |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC** **Soils Laboratory CSE Soils Laboratory**

**…………………… ……………….**