

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.965/35/L/10 Date: 22nd November, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **1. Customer’s Details:** NARIANA ENTERPRISES LIMITED.  **E-mail: technical@nariana.co.ke**  **Address:** P.O BOX 38318-00623 NRB Phone: 0721249576  **2. Customer Contact:** 0721249576 6. Job Card No. 1189/S/2023  **3. Sample Description:** Gravel 7. Date fee paid: 09/11/2023  **4. Sampled by:** Client. 8. GOK MR No.4388539  **5. Date Sample received:** 08/11/2023 9. Date Analysis started:16/11/2023  **10. Additional information provided by the customer:** Premier food Industries Access Road.  **Source:** Stockpile.   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | TEST RESULTS | | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Dosage** % | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | % Passing BS Sieve Size (mm) | | | | | | LL | PL | PI | LS | PM | MDD | OMC | 4days Soak  (%) | Swell | | 20 | 10 | 5 | 2 | 0.425 | 0.075 | % | % | % | % |  | Kg/m3 | ( % ) | (%) | | 765/S/23 | Gravel | Neat | 100 | 89 | 70 | 50 | 36 | 30 | 43 | 29 | 14 | 7 | 504 | 1646 | 21.0 | 25 | 0.3 | | **SOIL COMPOSITION: Gravel = 50%, Sand = 20%, Silt/clay =30%** | | | | | | | | | | | | | | | |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**

**OiC Soils Laboratory. CSE Soils Laboratory.**

**………………………. ………………………..**