

**REPUBLIC OF KENYA**

**MINISTRY OF ROADS AND TRANSPORT**

**STATE DEPARTMENT OF ROADS**

Telegraphic Address: “MINWORKS”, Nairobi Materials Testing & Research Division Telephone: Nairobi 0202554950 Machakos Road, Industrial Area Fax: 554877 P.O. Box 11873 – 00400 E-mail: [chiefengineer@mtrd.go.ke](mailto:chiefengineer@mtrd.go.ke) **NAIROBI**

Ref No. M.629/35/L/10 Date:28th September, 2023

|  |
| --- |
| **Laboratory Test Report** |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. **Customer’s Details:** LUKIN ENTERPRISES LIMITED.   **E-mail:** Not provided  **Address:** Not provided Phone: 0721515815  **2. Customer Contact:** 0721515815 6. Job Card No.750/S/2023  **3. Sample Description:** Gravel 7. Date fee paid: 22/09/2023  **4. Sampled by:** CLIENT. 8. GOK MR No.4058960  **5. Date Sample received:** 22/08/2023 9. Date Analysis started: 22/09/2023  **10. Additional information provided by the customer:** Access to kamulu police station  **Source:** Site   |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | |  | **TEST RESULTS** | | | | | | | | | | | | | | | | | **Sample No.** | **Reference** | **Grading** | | | | | | **Atterberg Limits** | | | | | **Compaction T180** | | **CBR** | | | **% Passing BS Sieve Size (mm)** | | | | | | **LL** | **PL** | **PI** | **LS** | **PM** | **MDD** | **OMC** | **4days Soak**  **(%)** | **Swell** | | **20** | **10** | **5** | **2** | **0.425** | **0.075** | **%** | **%** | **%** | **%** |  | **Kg/m3** | **( % )** | **(%)** | | 340/S/23 | Gravel | 100 | 90 | 59 | 48 | 41 | 31 | 38 | 24 | 14 | 7 | 574 | 1650 | 16.5 | 30 | 0.3 | | **SOIL COMPOSITION: Gravel =35%, Sand =30%, Silt/clay =35%** | | | | | | | | | | | | | | | |

|  |
| --- |
|  |

**Eng. J. M. Mbarua**

**For: CHIEF ENGINEER (MATERIALS)**